## Slide 1
Aging test of glass and MRPC
Outline:
  aging test of glass
aging test of MRPC
Conclusions
  Wang Yi
Department of Engineering Physics, Tsinghua University

## Slide 2
Aging test of low resistive glass
This glass was applied with 1000V for about 32days, integrated charge: 1 C/cm2
--roughly corresponding to the CBM life-time over 5 years operation at the maximum particle rate.
Glass specifications:

## Slide 3
3
Comparasion with other material
Morales talk @RPC2012

## Slide 4
Electrode Material Samples
sample | material | length [cm] | width [cm] | area [cm²] | thickness [cm] | volume [cm³] | weigth [g] | density [g/cm³]
layer-1 | soda-lime glass | 4 | 4 | 16 | 0.05 | 0.8 | 2.0 | 2.5
layer-2 | Si3N4 / SiC ceramics | 5 | 5 | 25 | 0.20 | 5.0 | 16.0 | 3.2
layer-3 | semicond. glass | 3 | 3 | 9 | 0.07 | 0.6 | 1.6 | 2.5

## Slide 5
Cyclotron U-120M (Řež)
Proton energy 36 MeV
Neutron production target Be
Neutron flux 108 - 1010 n/cm2/s
Neutron energy spectra 1 – 36 MeV
Experimental Facility
target support
Special thanks to A. Kugler and
O. Svoboda for their strong support.
Neutron energy spectrum

## Slide 6
6
Test result

## Slide 7
Hign rate MRPC
X-ray Generator
130cm
60cm
Setup of irradiation test
This is online test system. The efficiency and time resolution can be obtained by cosmic ray while irradiated by X-rays. 0.1C/cm2 charge is accumulated in 35 days.

## Slide 8
Current VS. X ray strength
Counting rate VS. X ray strength

## Slide 9
Efficiency VS. X ray strength
Efficiency VS. dosage
Efficiency

## Slide 10
Current

## Slide 11
Counting rate

## Slide 12
Charge spectrum
Before irradiation
First ten days
Second ten days
Third ten days

## Slide 13
Time resolution

## Slide 14
Conclusions
From high voltage, neutron test, we did not find any aging problem for low resistive glass.
We also studied the long term stability of high rate MRPC. 0.1C/cm2 charge is accumulated.

## Slide 15
Thanks for your attention !