## Slide 1
Update on SoLID-TOF
Outline:
  Conceptual design of SoLID-TOF
  Beam test @Hall A
  Aging test of glass and MRPC
  Development of 20ps MRPC
  Conclusions
  Wang Yi
Department of Engineering Physics, Tsinghua University

## Slide 2
Main requirements for TOF
The MRPC is developed for the TOF of SoLID
Main Requirements for TOF:
  /k separation up to 2.5GeV/c
  Time resolution < 100ps
  Rate capability > 10kHz/cm²
To separate very few K from , we require the TOF time resolution as good as possible.
We have to improve the time resolution to about 20ps.

## Slide 3
Conceptual design of SOLID-TOF
MRPC TOF wall we designed contain 150 MRPC modules in total, with 50 gas boxes and 3 counters in each box, covering the area of 10m².
MRPC1
MRPC2
MRPC3
100cm
16cmm
28cm
Total channel ~3600

## Slide 4
Volume resistivity: ~1010.cm
363mm
219mm
171mm
25mm
 | Length/mm | Width/mm | Thickness/mm
Gas gap | - | - | 0.25×10
Inner glass | 320 | 130-171 | 0.7
Outer glass | 330 | 138-182 | 1.1
Mylar | 335 | 153-198 | 0.18
Inner PCB | 350 | 182-228 | 1.6
Outer PCB | 350 | 172-218 | 0.8
Honeycomb | 330 | 153-198 | 6
Material dimensions
A MRPC prototype for SoLID-TOF

## Slide 5
Cosmic test
Cosmic ray test@Tsinghua August, 2011
Efficiency > 95% @ 96kV/cm (6.0kV)
Time resolution: ~ 52ps
PMT3
PMT4
PMT0
PMT2
PMT1
MRPC
Cosmic Ray Muon

## Slide 6
Beam test @ Hall A
Shield
High Energy e-
Top View
PMT1
PMT2
PMT3
PMT4
PMT0
Target
Target
Test setup
The diagram of DAQ system

## Slide 7
Rate Performance
Voltage: 6800V
Flux:11kHz/cm²
Efficiency:~95%
Time Resolution: 78ps
Flux:16kHz/cm²
Efficiency:~95%
Time Resolution: 82ps

## Slide 8
Charge spectrum at different rate
Charge Distribution
Base Line
Signal
Significant reduction of charge distribution can be seen as the background rate increases.
The reduction of electrical field is caused mainly by both background irradiation and electron beams.
Rate capability of the counter is higher than 16kHz/cm².

## Slide 9
Aging test of low resistive glass
This glass was applied with 1000V for about 32days, integrated charge: 1 C/cm2
--roughly corresponding to the CBM life-time over 5 years operation at the maximum particle rate.
Glass specifications:

## Slide 10
10
10
10
Comparasion with other material
Morales talk @RPC2012

## Slide 11
Cyclotron U-120M (Řež)
Proton energy 36 MeV
Neutron production target Be
Neutron flux 108 - 1010 n/cm2/s
Neutron energy spectra 1 – 36 MeV
Neutron Test
target support
Neutron energy spectrum

## Slide 12
12
Hign rate MRPC
X-ray Generator
130cm
60cm
Online irradiation test
This is online test system. The efficiency and time resolution can be obtained by cosmic ray while irradiated by X-rays. 0.1C/cm2 charge is accumulated in 35 days.

## Slide 13
Efficiency plateau before and after irradiation

## Slide 14
Variation of efficiency, cluster size and noise with irradiation time
Variation of time resolution with irradiation time

## Slide 15
TOF electronics
Fast preamplifier：
Ninos (TOT) (ALICE)
Padi (TOT) (GSI)
CAD (TOT) (Tsinghua)
Low time jitter faster FEE
TDC
HPTDC (ALICE, 25ps/ch)
GET4 (GSI, 25ps/ch)
FPGA TDC (GSI and other)
Pulse wave form digitizer
DAQ

## Slide 16
Intrinsic resolution of 10gap-MRPC
Time jitter of HPTDC 25ps
NINOs ASIC+Interface card 24ps
MRPC resolution tested 40ps
So the intrinsic resolution of MRPC is:

## Slide 17
17
Resolution of 24 x140m MRPC
Fast wave form digitizer 30-> 5ps
Low time jitter fast FEE 24-> 5ps
MRPC intrinsic 20-> 13ps
Time resolution of TOF:

## Slide 18
TOF PID at the EIC
TOF Positives
Compact (10-15 cm of space needed), allowing more room for, e.g., RICH
More clean PID
Can contribute to e/h identification using TPC dE/dx
TOF Negatives
Start counter?
@ 1m distance | Distance | Pion-Kaon Separation | Kaon-Proton Separation
σtot=100 ps | 1m |  | 
σtot=10 ps | 1m |  | 
σtot=10 ps | 3m |  | 
Momentum reach of TOF PID reaches interesting levels if one can achieve ~ 10 ps

## Slide 19
19
 | MRPC ( C. Williams et al. ) | MRPC ( UIUC & BNL)
Gas Gap Width | 160um (fishing line) | 105um (fishing line, and 165, 125, 75um)
# of Gas Gaps | 4 stack x 6 layers = 24 | 4 stack x 9 layers = 36
# of thin glass layers | 4 stacks x 5 layers = 20 (250um thick glass) | 4 stack x 8 layers = 32 (210um thick glass)
Preamplifier | Differential type, NINO chip | LMH6881 2.8-GHz + Evaluation Board
TDC and DAQ | Oscilloscope (10Gs) | DRS4-V5(5Gs) + PC
Time resolution | 20 ps published (16 ps private comm) | 18ps
Configuration of eRD10 Prototype mRPC
Gas gap width : 160um
(16ps timing resolution)
Gas gap width : 105um
Crispin Williams
BNL&UIUC Prototype
4 x
4 x
PCB
glass
Gas gap

## Slide 20
20
Time Resolution Measurement at UIUC
MRPC-A
MRPC-B
DRS4-V5
(Wave form digitizer)
PC
(DAQ)
DC0,1,2
SC1
SC4
preamp
preamp
Gas Cylinder
USB
50 Ohm cable (<1m)
ch2
ch2
Muon trigger
Gas Mixture : “Freon” (R134a) 90% : Iso 5% : SF6 5%
SC2
SC3
DC3,4
Pb Block

## Slide 21
21
Difference between time of top and bottom mRPC, Δt = t2 – t1= 25 ps
  σt = Δt/√2 = 18 ps
  Used a “Leading Edge Discriminator technique” in software from waveform, slew corrected
  Difference in pathlength taken into account
  Wings possibly due to noise, cross-talk, streamers, or something else?
We believe best published result is 20 ps
  Nucl.Instrum.Meth. A594 (2008) 39-43
  Nucl.Instrum.Meth. A629 (2011) 106-110
Time resolution

## Slide 22
22
15Ghz wave form digitizer
Rising edge time<1ns, more than 10 sampling point which can keep the shape of rising edge.

## Slide 23
ground
ground
+HV
-HV
+HV
-HV
+HV
Structure of new MRPC
Gas gap: 105μm
Gap number: 32
Glass thickness: 0.35mm
Honey comb plate
PCB
Mylar
Carbon electrode
Glass

## Slide 24
Test signal input
MRPC signal input
Time output
Charge output
Power circuit
MRPC signal -- Time
MRPC signal -- Charge
PMT Coincindence
Possible FEE and pulse sampling digitizer
CAEN DT5742:16 channel, 5Ghz, 12bit sampling

## Slide 25
Next to do
Assemble the narrow gap MRPC
Cosmic test
Beam test at IHEP or SPS
Possible using fast FEE and 15GSa/s TDC (DRS4)
T.O.B

## Slide 26
Conclusions
A SoLID-TOF MRPC prototype is developed, its time resolution is 75ps, rate capability reach 16kHz/cm2.
From high voltage and neutron radiation test, we did not find any aging problem for low resistive glass. We also studied the long term stability of the MRPC. 0.1C/cm2 charge is accumulated. No obvious performance degradation is observed.
MRPC intrinsic resolution can reach 13ps. Fast FEE and high band width wave form digitizer has to be used to improve TOF resolution -> 20ps.

## Slide 27
Thanks for your attention !